## Slide 1
在此处键入公式。
Introduction
Lean Li1, Yue Chen1, Haoran Chen1, Yizi Feng1,
Yuanfei Fan1,Yan Huang1, Zhe Yuan3, Yizheng Wu1
*Email: 25110190049@m.fudan.edu.cn
1Department of Physics, State Key Laboratory of Surface Physics, Fudan University, Shanghai 200433, China
2Center for Advanced Quantum Studies and Department of Physics, Beijing Normal University, Beijing 100875, China
Summary
Anisotropic High-Order Anomalous Hall Effect in Epitaxial Nickel Thin Films
residual
Anomalous Hall effect
High-order AHE harmonics up to 19th order in Ni(001)
In-plane-sensitive AHE beyond the conventional Mz​ picture
Fourfold anisotropy visualized by full 3D angular mapping
Distinct temperature evolution of two AHE components
3D angular mapping of anisotropic AHE
Observation of anisotropic angular-dependent AHE
Ni(20 nm)/LAO(001)
Measurement geometry:
AHE contains an in-plane-sensitive component
T=5 K
T=300 K
AHE always proportional to Mz？
High-order AHE from multipolar response
Can high-order AHE harmonics carry in-plane crystalline anisotropy?
High order
Spin-orbit coupling
High order
Spin-dependent transport
W. Peng et al., arXiv:2402.15741 (2024)
In-plane AHE: evidence beyond Mz
(AHE)
Beyond Mz-proportional AHE？
In-plane anomalous Hall effect
+
Ordinary Hall
Anomalous Hall
Anisotropy enhanced in 5K
Multi-cycle angular measurement
Extraction of intrinsic AHE and high-order harmonics
Ordinary Hall Subtraction
Up to 19-fold AHE
Muti field verification
AHE curves nearly collapse
Fourier verification of high-order AHE
Multi-cycle angular measurement
Fast Fourier transformation
High-order expansion of AHE
Phenomenological model of AHE based on crystal symmetry
W. Döring, Ann. Phys. 424, 259 (1938)
Onsager relation：
Cubic crystalline symmetry
From Ohm’s law , expansion of on :
Temperature evolution of anisotropic high-order AHE
Conventional AHE
W. Peng et al., arXiv:2402.15741 (2024)
Liu et al., Phys. Rev. X 15, 031006 (2025).
Temperature dependence of separated AHE components
: polar component
: Fourfold anisotropic component
Polar and in-plane-sensitive AHE components exhibit distinct temperature evolution.
3D full mapping of Ni(001) AHE
T=300 K
T=5 K
5K:Fourfold in-plane Symmetry
​-dependent AHE confirmed by DFT
Global fitting by symmetry model​
OHE-subtracted AHE reveals robust odd-order harmonics up to 19 fold beyond the conventional Mz picture.
Symmetry-model fitting formula
300K:Weak anisotropic
Full 3D angular mapping visualizes fourfold crystalline anisotropy in high-order AHE.
Both polar and anisotropic AHE host high-order harmonics.
Beyond the conventional Mz​ picture.