## Slide 1
Magnetic Order in the van der Waals magnet VCl3
Zeyu Kao,1 Yiqing Hao,2 Yimeng Gu,1 Lixing Chen,1 Enkang Zhang,1 Hao Zhang,1 Fabio Orlandi,3 Pascal Manuel,3
Junfeng Wang,4 Chao Dong,4 Chuanying Xi,5 Zefeng Chen,6 Changsong Xu,6 and Jun Zhao1,7,*
1State Key Laboratory of Surface Physics and Department of Physics, Fudan University, Shanghai 200433, China
2Neutron Scattering Division, Oak Ridge National Laboratory, Oak Ridge, Tennessee 37831, USA
3ISIS Pulsed Neutron and Muon Source, Science and Technology Facility Council, Rutherford Appleton Laboratory, Harwell Campus, Didcot OX11 0QX, United Kingdom
4Wuhan National High Magnetic Field Center and School of Physics, Huazhong University of Science and Technology, Wuhan 430074, China
5Anhui Key Laboratory of Low-Energy Quantum Materials and Devices, High Magnetic Field Laboratory, HFIPS, Chinese Academy of Sciences, Hefei, Anhui 230031, China
6Key Laboratory of Computational Physical Sciences (Ministry of Education), Institute of Computational Physical Sciences, State Key Laboratory of Surface Physics, and Department of Physics, Fudan University, Shanghai 200433, China
7Institute of Nanoelectronics and Quantum Computing, Fudan University, Shanghai 200433, China
Abstract
VCl3 is a newly synthesized layered van der Waals magnet in the vanadium trihalide family. Using high-quality single crystals, we combined thermodynamic measurements, magnetization, and single-crystal neutron diffraction to determine its structural and magnetic properties. VCl3 crystallizes
crystallizes in a BiI3-type structure at room temperature and undergoes a structural phase transition at TS = 103.7 K, followed by antiferromagnetic ordering below TN = 21.8 K. Neutron diffraction identifies a zigzag antiferromagnetic ground state with propagation vector k = (0, 0.5, 1). The ordered V3+ moments are mainly oriented along the c axis but are canted by about 21° toward the a axis, giving a total ordered moment of 1.09 μB per V3+. Field-dependent magnetization reveals strong anisotropy and a plateau-like feature near half magnetization for fields along the c axis, indicating an unconventional field-induced magnetic phase. These findings establish VCl3 as a promising platform for exploring anisotropic magnetism and field-tunable phases in vanadium-based honeycomb magnets.
Single crystal structure
Schematic illustrations of the crystal structure of VCl3 viewed along the (a) a axis and (b) c axis. (c) Photograph of a high-quality VCl3 single crystal. (d) X-ray diffraction pattern of the cleaved surface measured at room temperature. The inset shows the rocking curve of the (0, 0, 6) reflection. (e) X-ray Laue diffraction pattern taken along the c axis.
Structural and magnetic phase transition
(a) Heat capacity measured from 95 to 115 K as a function of temperature. (b) Temperature dependence of the Bragg peak (2, 2, 0). The heat map was generated using raw data from scans of the (2, 2, 0) peak at temperatures ranging from 5 to 130 K with an interval of 5 K. (c) Magnetic susceptibility measured from 1.8 to 300 K under an external field of 500 Oe. The inset provides a zoomed-in view of the structural phase transition. (d) Low-temperature heat capacity under external magnetic fields along the c axis and a axis.
Neutron diffraction taken on single crystal VCl3 at HB-3A, HFIR.
(a) and (b) A high- and low-temperature comparison of two representative inequivalent magnetic Bragg peaks, highlighting the emergence of magnetic intensity at low temperature. (c) Temperature comparison of the (0, 1.5, 0) peak, which shows negligible change, indicating that the signal is a spurious reflection arising from half-wavelength neutrons rather than a magnetic origin. (d) Neutron diffraction mapping of the (0, K, L) reciprocal plane at the base temperature obtained on HB-3A, ORNL, revealing a distinct set of magnetic Bragg peaks.
Magnetic structure and magnetization measurement
(a) Overall illustration of the zigzag antiferromagnetic structure of VCl3 as determined by least squares refinement. The total ordered moment is 1.09(2) µB. (b) Magnetization curve obtained from laboratory-based vibrating sample magnetometry (VSM), steady high magnetic field measurements (SF), and pulsed field experiments (PF) under external magnetic fields along the c axis and a axis. The inset shows the raw derivative data from the pulsed field measurement, where a clear two-step transition is observed.
Zeyu Kao, et al. Phys. Rev. B 113, 094428 (2026). (Editors’ Suggestion）
(a)
(b)
(a)
(b)
(c)
(d)
(e)
(a)
(b)
(c)
(d)
(a)
(b)
(c)
(d)