## Slide 1
Dynamic Properties of Exchange Spirals in Fe/CoO
Bilayer with Strong Interfacial Exchange Coupling
Yuanfei Fan, Hongyue Xu, Tong Wu, Yizheng Wu*
Department of Physics, Fudan University, Shanghai, China
Angular-dependent dynamic properties
Simulation of spin dynamics
In-plane FMR measurements
Conclusion
Exchange spirals were studied by ferromagnetic resonance (FMR).
The structure of exchange spirals was confirmed by micromagnetic simulation and PNR.
Spin-wave excitation modes of spirals with different structures were simulated.
Background & Motivation
Exchange spiral in FM/AFM
A. Frisk, et al. Phys. Rev. Applied (2023)
Magnetic exchange spirals
Spin dynamics of exchange spirals
Experimental methods and theory
Basic theory
Interfacial exchange coupling → unique dynamic properties
Unidirectional asymmetry
Dynamic response of exchange spiral
Non-uniform effective field Heff → Non-uniform precession dynamics
Exchange spirals
in Fe/CoO bilayer
FMR measurement
Strong interfacial exchange coupling
Spin dynamic properties in Fe/CoO?
300 K
50 K after field cooling
Hrot=0.4 T
Sweeping field
Rotating field
Hrot=0.4 T
H along x-axis
H along y-axis
Sweeping field
Rotating field
Hrot=0.3 T
Hrot=0.4 T
Canted standing spin-wave modes
Fe/CoO bilayer
Hard/soft FM bilayers
Spiral → frequency dip / linewidth anomaly / asymmetric switching
Layer-resolved precession modes
FMR spectrum
RHEED pattern
Micromagnetic simulation of exchange spirals
Interfacial exchange coupling (anisotropic field) → Exchange spiral
Structure of exchange spirals under different Hrot
Layer-resolved magnetization profiles
Simulation configuration
PNR characterization of exchange spirals
Non‑collinear spiral state
Anisotropic damping
Uniform precession model
ΔHFe//CoO ≫ ΔHFe⟂CoO
Direct evidence of the interfacial spiral
Asymmetric dissipation
Anisotropic interfacial dissipation
Chirality switching
Non‑collinear spiral state
θrot=2°
θrot=15°
CoO spin disorder
Non‑collinear spin structure
Spiral dynamics in FM/FM systems
Nonreciprocal spin-wave propagation
M. X. Jiang, et al. Phys. Rev. B (2025)
Unexplored spiral dynamics in FM/AFM
Q. Li, et al. Phys. Rev. B (2017)
M. Yang, et al. Phys. Rev. B (2020)
M. Dabrowski, et al. New J. Phys. (2021)
Py
[CO/Pt]n
Anisotropic damping in Fe/CoO
Magnetization depth profiles (spiral vs. uniform)
Nonreciprocal